# DAFTAR PUSTAKA

Amanto, H., & Daryanto. (2003). Ilmu Bahan. Bumi Aksara.

ASM. (2005). Properties and Selections: Irons Steels and High Performance Alloy - Vol 1.

Avner. (1974). INTRODUCTION TO PHYSICAL Second Edition (Second Edi). McGraw-Hill, Inc.

Bain, C. E. (1966). ALLOYING ELEMENTS IN STEEL (Second Edi). American Society For Metals.

Cardelli. (2008). Materials Handbook : A Concise Dekstop Reference. Elsevier.

Fan, J., Saragi, H. T., Qadry, A., Putra, E., Boangmanalu, D., Bahri, A., & Artikel, R. (2023). Pengaruh Temperatur Terhadap Kekuatan Impak Material Baja ST37 dengan Metode Charpy dan Izod. 6(2), 65–69.

George. E, D. (1961). Mechanical metallurgy. McGRAW-HILL BOOK COMPANY.

Groover, M. P. (2013). Fundamentals of Modern Manufacturing Material, Processes, and Systems, 5th Edition. In Journal of Chemical Information and Modeling.

Motomichi, Koyama Taekyung Lee b, Chong Soo Lee b, K. T. (2013). Grain refinement effect on cryogenic tensile ductility in a Fe–Mn–C twinning-induced plasticity steel. Material and Design, 49, 234–241. https://doi.org/https://doi.org/10.1016/j.matdes.2013.01.061

Seetharaman, S. (2014). TREATISE ON PROCESS METALLURGY INDUSTRIAL PROCESSES, Part A. Elsevier.

Simanjuntak, B. (2011). Pengaruh Konsentrasi Mangan (Mn) Sifat Mekanik Baja Karbon Rendah. Universitas Sumatera Utara.

Smith, F, W. (1994). STRUCTURE AND PROPERTIES OF ENGINEERING ALLOYS (2nd ed.). McGraw-Hill, Inc.

Soeleman, & Putra, M. I. H. (2008). Analisis Karakteristik Gear Sprocket Standard dan Racing Pada Sepeda Motor. Sintek, 2(2), 26–35. http://motor.otomotifnet.com

Song, Changjiang, Wenbin Xia a, Jun Zhang b, Yuanyi Guo a, Q. Z. a. (2013). Microstructure and mechanical properties of Fe-Mn based alloys sub-rapid solidification. Material and Design, 51, 262–267.

Surdia, T. (1999). PENGETAHUAN BAHAN TEKNIK (4th ed.). PRADNYA PARAMITA.

Tangstad, M. (2013). Manganese Ferroalloys Technology. In Handbook of Ferroalloys: Theory and Technology (pp. 221–265). Elsevier. https://doi.org/10.1016/B978-0-08-097753-9.00001-0

# LAMPIRAN

- Menghitung Kekerasan Brinnel

    - Pengolahan data kekerasan brinnel pada variasi penambahan FeMn 1,5% (1).

F = 187,5 Kgf

D = 2,5 mm

d = 0,806

Ditanya : BHN ..?

BHN= 2Fπ.D ( D-D2- d2)

BHN= 2. 187,53,14 .  2,5 ( 2,5-2,52- 0,8062)

BHN= 3757,85 ( 2,5-6,25- 0,649)

BHN= 3757,85 ( 2,5-5,601)

BHN= 3757,85 ( 2,5-2,367)

BHN= 3757,85 x 0,133

BHN= 3751,044

BHN = 351,9

    - Pengolahan data kekerasan brinnel pada variasi penambahan FeMn 1,5% (2).

F = 187,5 Kgf

D = 2,5 mm

d = 0,849

Ditanya : BHN ..?

BHN= 2Fπ.D ( D-D2- d2)

BHN= 2. 187,53,14 .  2,5 ( 2,5-2,52- 0,8492)

BHN= 3757,85 ( 2,5-6,25- 0,72)

BHN= 3757,85 ( 2,5-5,53)

BHN= 3757,85 ( 2,5-2,35)

BHN= 3757,85 x 0,15

BHN= 3751,177

BHN = 318,6

    - Pengolahan data kekerasan brinnel pada variasi penambahan FeMn 1,5% (3).

F = 187,5 Kgf

D = 2,5 mm

d = 0,829

Ditanya : BHN ..?

BHN= 2Fπ.D ( D-D2- d2)

BHN= 2. 187,53,14 .  2,5 ( 2,5-2,52- 0,8292)

BHN= 3757,85 ( 2,5-6,25- 0,687)

BHN= 3757,85 ( 2,5-5,563)

BHN= 3757,85 ( 2,5-2,358)

BHN= 3757,85 x 0,142

BHN= 3751,144

BHN = 327,7

    - Pengolahan data kekerasan brinnel pada variasi penambahan FeMn 2% (1).

F = 187,5 Kgf

D = 2,5 mm

d = 0,741

Ditanya : BHN ..?

BHN= 2Fπ.D ( D-D2- d2)

BHN= 2. 187,53,14 .  2,5 ( 2,5-2,52- 0,7412)

BHN= 3757,85 ( 2,5-6,25- 0,549)

BHN= 3757,85 ( 2,5-5,701)

BHN= 3757,85 ( 2,5-2,387)

BHN= 3757,85 x 0,113

BHN= 3750,887

BHN = 422,7

    - Pengolahan data kekerasan brinnel pada variasi penambahan FeMn 2% (2).

F = 187,5 Kgf

D = 2,5 mm

d = 0,738

Ditanya : BHN ..?

BHN= 2Fπ.D ( D-D2- d2)

BHN= 2. 187,53,14 .  2,5 ( 2,5-2,52- 0,7382)

BHN= 3757,85 ( 2,5-6,25- 0,544)

BHN= 3757,85 ( 2,5-5,706)

BHN= 3757,85 ( 2,5-2,388)

BHN= 3757,85 x 0,112

BHN= 3750,879

BHN = 426,6

- Pengolahan data kekerasan brinnel pada variasi penambahan FeMn 2% (3).

F = 187,5 Kgf

D = 2,5 mm

d = 0,777

Ditanya : BHN ..?

BHN= 2Fπ.D ( D-D2- d2)

BHN= 2. 187,53,14 .  2,5 ( 2,5-2,52- 0,7772)

BHN= 3757,85 ( 2,5-6,25- 0,603)

BHN= 3757,85 ( 2,5-5,647)

BHN= 3757,85 ( 2,5-2,376)

BHN= 3757,85 x 0,124

BHN= 3750,973

BHN = 385,4

- Pengolahan data kekerasan brinnel pada variasi penambahan FeMn 2,5% (1).

F = 187,5 Kgf

D = 2,5 mm

d = 0,724

Ditanya : BHN ..?

BHN= 2Fπ.D ( D-D2- d2)

BHN= 2. 187,53,14 .  2,5 ( 2,5-2,52- 0,7242)

BHN= 3757,85 ( 2,5-6,25- 0,524)

BHN= 3757,85 ( 2,5-5,726)

BHN= 3757,85 ( 2,5-2,392)

BHN= 3757,85 x 0,108

BHN= 3750,847

BHN = 442,7

- Pengolahan data kekerasan brinnel pada variasi penambahan FeMn 2,5% (2).

F = 187,5 Kgf

D = 2,5 mm

d = 0,751

Ditanya : BHN ..?

BHN= 2Fπ.D ( D-D2- d2)

BHN= 2. 187,53,14 .  2,5 ( 2,5-2,52- 0,7512)

BHN= 3757,85 ( 2,5-6,25- 0,564)

BHN= 3757,85 ( 2,5-5,686)

BHN= 3757,85 ( 2,5-2,384)

BHN= 3757,85 x 0,116

BHN= 3750,910

BHN = 412,08

- Pengolahan data kekerasan brinnel pada variasi penambahan FeMn 2,5% (3).

F = 187,5 Kgf

D = 2,5 mm

d = 0,716

Ditanya : BHN ..?

BHN= 2Fπ.D ( D-D2- d2)

BHN= 2. 187,53,14 .  2,5 ( 2,5-2,52- 0,7162)

BHN= 3757,85 ( 2,5-6,25- 0,512)

BHN= 3757,85 ( 2,5-5,738)

BHN= 3757,85 ( 2,5-2,395)

BHN= 3757,85 x 0,105

BHN= 3750,824

BHN = 455,09

- Menghitung Uji Tarik

    - Pengolahan data uji tarik pada variasi penambahan FeMn 1,5% (1).

σ = PmaxAo

Menghitung kekutan tarik:

Pmax		= 42,72757 KN

= 42,72757 x 1000

= 42727,57 N

Mencari diameter (Do) spesimen menggunakan rumus:

Ao 		= π4  x D02

122,720	= 3,144 x Do2

122,720 x 4	= 3,14 x Do2

490,883,14		= Do2

156,331	= Do2

Do		= 156,331

Do		= 12,50323 mm

Mencari tegangan tarik:

σ 	= PmaxAo

= 42727,57 122,720

= 348,17 MPa

    - Pengolahan data uji tarik pada variasi penambahan FeMn 1,5% (2).

σ = PmaxAo

Menghitung kekutan tarik:

Pmax		= 35,86292 KN

= 35,86292 x 1000

= 35862,92 N

Mencari diameter (Do) spesimen menggunakan rumus:

Ao 		= π4  x D02

122,721	= 3,144 x Do2

122,721 x 4	= 3,14 x Do2

490,8843,14	= Do2

156,332	= Do2

Do		= 156,332

Do		= 12,50327 mm

Mencari tegangan tarik:

σ 	= PmaxAo

= 35862,92 122,721

= 292,23 MPa

    - Pengolaham data uji tarik pada variasi penambahan FeMn 2% (1).

σ = PmaxAo

Menghitung kekutan tarik:

Pmax		= 29,72396 KN

= 29,72396 x 1000

= 29723,96 N

Mencari diameter (Do) spesimen menggunakan rumus:

Ao 		= π4  x D02

122,719	= 3,144 x Do2

122,719 x 4	= 3,14 x Do2

490,8763,14	= Do2

156,329	= Do2

Do		= 156,329

Do		= 12,50315 mm

Mencari tegangan tarik:

σ 	= PmaxAo

= 29723,96 122,719

= 242,21 MPa

    - Pengolahan data uji tarik pada variasi penambahan FeMn 2% (2).

σ = PmaxAo

Menghitung kekutan tarik:

Pmax		= 29,81222 KN

= 29,81222 x 1000

= 29812,22 N

Mencari diameter (Do) spesimen menggunakan rumus:

Ao 		= π4  x D02

122,719	= 3,144 x Do2

122,719 x 4	= 3,14 x Do2

490,8763,14	= Do2

156,329	= Do2

Do		= 156,329

Do		= 12,50315 mm

Mencari tegangan tarik:

σ 	= PmaxAo

= 29812,22122,719

= 242,93 MPa

    - Pengolahan data uji tarik pada variasi penambahan FeMn 2,5% (1).

σ = PmaxAo

Menghitung kekutan tarik:

Pmax		= 33,49952 KN

= 33,49952 x 1000

= 33499,52 N

Mencari diameter (Do) spesimen menggunakan rumus:

Ao 		= π4  x D02

122,744	= 3,144 x Do2

122,744 x 4	= 3,14 x Do2

490,9793,14		= Do2

156,361	= Do2

Do		= 156,361

Do		= 12,50443 mm

Mencari tegangan tarik:

σ 	= PmaxAo

= 33499,52 122,744

= 272,98 MPa

    - Pengolahan data uji tarik pada variasi penambahan FeMn 2,5% (2).

σ = PmaxAo

Menghitung kekutan tarik:

Pmax		= 29,38072 KN

= 29,38072 x 1000

= 29380,72 N

Mencari diameter (Do) spesimen menggunakan rumus:

Ao 		= π4  x D02

122,721	= 3,144 x Do2

122,721 x 4	= 3,14 x Do2

490,8843,14	= Do2

156,332	= Do2

Do		= 156,332

Do		= 12,50327 mm

Mencari tegangan tarik:

σ 	= PmaxAo

= 29380,72 122,721

= 239,41 MPa

- Menghitung Uji Impact (Charpy)

    - Pengolahan data uji impact pada raw material (1).

Lebar benda uji (ℓ)		= 10,85 mm

Tebal benda uji (t)		= 10,52 mm

Panjang pendulum (R)	= 0,8 m

Berat pendulum (G)	= 30 kg x 9,8 = 294,3 N

Cos α			= 90º	= 0

Cos β			= 82º	= 0,1391

Mencari luas penampang:

Ao	= ℓ x t

= 10,85 x 10,52

= 114,142 mm2

Rumus energi yang diserap benda uji/tenaga patah:

E 	= G x R ( Cos β - Cos α )

E	= 294,3 x 0,8 ( 0,1391 – 0 )

E 	= 235,44 x 0,1391

E 	= 32,7 J

Rumus Harga Impak (HI):

HI	= EA

= 32,7114,142

= 0,286 J/mm2

    - Pengolahan data uji impact pada raw material (2).

Lebar benda uji (ℓ)		= 11,02 mm

Tebal benda uji (t)		= 10,43 mm

Panjang pendulum (R)	= 0,8 m

Berat pendulum (G)	= 30 kg x 9,8 = 294,3 N

Cos α			= 90º	= 0

Cos β			= 83º	= 0,1218

Mencari luas penampang:

Ao	= ℓ x t

= 11,02 x 10,43

= 114,938 mm2

Rumus energi yang diserap benda uji/tenaga patah:

E 	= G x R ( Cos β - Cos α )

E	= 294,3 x 0,8 ( 0,1218 – 0 )

E 	= 235,44 x 0,1218

E 	= 28,6 J

Rumus Harga Impak (HI):

HI	= EA

= 28,6114,938

= 0,248 J/mm2

    - Pengolahan data uji impact pada raw material (3).

Lebar benda uji (ℓ)		= 10,97 mm

Tebal benda uji (t)		= 10,12 mm

Panjang pendulum (R)	= 0,8 m

Berat pendulum (G)	= 30 kg x 9,8 = 294,3 N

Cos α			= 90º	= 0

Cos β			= 82º	= 0,1391

Mencari luas penampang:

Ao	= ℓ x t

= 10,97 x 10,12

= 111,016 mm2

Rumus energi yang diserap benda uji/tenaga patah:

E 	= G x R ( Cos β - Cos α )

E	= 294,3 x 0,8 ( 0,1391 – 0 )

E 	= 235,44 x 0,1391

E 	= 32,7 J

Rumus Harga Impak (HI):

HI	= EA

= 32,7111,016

= 0,276 J/mm2

    - Pengolahan data uji impact pada variasi penambahan FeMn 1,5% (1).

Lebar benda uji (ℓ)		= 11,22 mm

Tebal benda uji (t)		= 10,87 mm

Panjang pendulum (R)	= 0,8 m

Berat pendulum (G)	= 30 kg x 9,8 = 294,3 N

Cos α			= 90º	= 0

Cos β			= 85º	= 0,0871

Mencari luas penampang:

Ao	= ℓ x t

= 11,22 x 10,87

= 121,961 mm2

Rumus energi yang diserap benda uji/tenaga patah:

E 	= G x R ( Cos β - Cos α )

E	= 294,3 x 0,8 ( 0,0871 – 0 )

E 	= 235,44 x 0,0871

E 	= 20,5 J

Rumus Harga Impak (HI):

HI	= EA

= 20,5121,961

= 0,168 J/mm2

    - Pengolahan data uji impact pada variasi penambahan FeMn 1,5% (2).

Lebar benda uji (ℓ)	= 10,57 mm

Tebal benda uji (t)		= 9,84 mm

Panjang pendulum (R)	= 0,8 m

Berat pendulum (G)	= 30 kg x 9,8 = 294,3 N

Cos α			= 90º	= 0

Cos β			= 84,5º	= 0,095

Mencari luas penampang:

Ao	= ℓ x t

= 10,57 x 9,84

= 104,008 mm2

Rumus energi yang diserap benda uji/tenaga patah:

E 	= G x R ( Cos β - Cos α )

E	= 294,3 x 0,8 ( 0,095 – 0 )

E 	= 235,44 x 0,095

E 	= 22,3 J

Rumus Harga Impak (HI):

HI	= EA

= 22,3104,008

= 0,2134 J/mm2

    - Pengolahan data uji impact pada variasi penambahan FeMn 1,5% (3).

Lebar benda uji (ℓ)	= 10,09 mm

Tebal benda uji (t)		= 10,10 mm

Panjang pendulum (R)	= 0,8 m

Berat pendulum (G)	= 30 kg x 9,8 = 294,3 N

Cos α			= 90º	= 0

Cos β			= 85º	= 0,0871

Mencari luas penampang:

Ao	= ℓ x t

= 10,09 x 10,10

= 101,909 mm2

Rumus energi yang diserap benda uji/tenaga patah:

E 	= G x R ( Cos β - Cos α )

E	= 294,3 x 0,8 ( 0,0871 – 0 )

E 	= 235,44 x 0,0871

E 	= 20,5 J

Rumus Harga Impak (HI):

HI	= EA

= 20,5101,909

= 0,194 J/mm2

    - Pengolahan data uji impact pada variasi penambahan FeMn 2% (1).

Lebar benda uji (ℓ)	= 10,65 mm

Tebal benda uji (t)		= 10,84 mm

Panjang pendulum (R)	= 0,8 m

Berat pendulum (G)	= 30 kg x 9,8 = 294,3 N

Cos α			= 90º	= 0

Cos β			= 84,75º	= 0,0915

Mencari luas penampang:

Ao	= ℓ x t

= 10,65 x 10,84

= 115,446 mm2

Rumus energi yang diserap benda uji/tenaga patah:

E 	= G x R ( Cos β - Cos α )

E	= 294,3 x 0,8 ( 0,0915 – 0 )

E 	= 235,44 x 0,0915

E 	= 21,5 J

Rumus Harga Impak (HI):

HI	= EA

= 21,5115,446

= 0,186 J/mm2

    - Pengolahan data uji impact pada variasi penambahan FeMn 2% (2).

Lebar benda uji (ℓ)	= 10,35 mm

Tebal benda uji (t)		= 10,05 mm

Panjang pendulum (R)	= 0,8 m

Berat pendulum (G)	= 30 kg x 9,8 = 294,3 N

Cos α			= 90º	= 0

Cos β			= 85º	= 0,0871

Mencari luas penampang:

Ao	= ℓ x t

= 10,35 x 10,05

= 104,017 mm2

Rumus energi yang diserap benda uji/tenaga patah:

E 	= G x R ( Cos β - Cos α )

E	= 294,3 x 0,8 ( 0,0871 – 0 )

E 	= 235,44 x 0,0871

E 	= 20,5 J

Rumus Harga Impak (HI):

HI	= EA

= 20,5104,017

= 0,197 J/mm2

    - Pengolahan data uji impact pada variasi penambahan FeMn 2% (3).

Lebar benda uji (ℓ)	= 10,5 mm

Tebal benda uji (t)		= 9,85 mm

Panjang pendulum (R)	= 0,8 m

Berat pendulum (G)	= 30 kg x 9,8 = 294,3 N

Cos α			= 90º	= 0

Cos β			= 85,2º	= 0,0836

Mencari luas penampang:

Ao	= ℓ x t

= 10,5 x 9,85

= 103,425 mm2

Rumus energi yang diserap benda uji/tenaga patah:

E 	= G x R ( Cos β - Cos α )

E	= 294,3 x 0,8 ( 0,0836 – 0 )

E 	= 235,44 x 0,0836

E 	= 19,6 J

Rumus Harga Impak (HI):

HI	= EA

= 19,6103,425

= 0,190 J/mm2

    - Pengolahan data uji impact pada variasi penambahan FeMn 2,5% (1).

Lebar benda uji (ℓ)	= 11,05 mm

Tebal benda uji (t)		= 10,58 mm

Panjang pendulum (R)	= 0,8 m

Berat pendulum (G)	= 30 kg x 9,8 = 294,3 N

Cos α			= 90º	= 0

Cos β			= 85,6º	= 0,0767

Mencari luas penampang:

Ao	= ℓ x t

= 11,05 x 10,58

= 116,909 mm2

Rumus energi yang diserap benda uji/tenaga patah:

E 	= G x R ( Cos β - Cos α )

E	= 294,3 x 0,8 ( 0,0767 – 0 )

E 	= 235,44 x 0,0767

E 	= 18,05 J

Rumus Harga Impak (HI):

HI	= EA

= 18,05116,909

= 0,154 J/mm2

    - Pengolahan data uji impact pada variasi penambahan FeMn 2,5% (2).

Lebar benda uji (ℓ)	= 10,80 mm

Tebal benda uji (t)		= 10,42 mm

Panjang pendulum (R)	= 0,8 m

Berat pendulum (G)	= 30 kg x 9,8 = 294,3 N

Cos α			= 90º	= 0

Cos β			= 85º	= 0,0871

Mencari luas penampang:

Ao	= ℓ x t

= 10,80 x 10,42

= 112,536 mm2

Rumus energi yang diserap benda uji/tenaga patah:

E 	= G x R ( Cos β - Cos α )

E	= 294,3 x 0,8 ( 0,0871 – 0 )

E 	= 235,44 x 0,0871

E 	= 20,5 J

Rumus Harga Impak (HI):

HI	= EA

= 20,5112,536

= 0,182 J/mm2

    - Pengolahan data uji impact pada variasi penambahan FeMn 2,5% (3).

Lebar benda uji (ℓ)	= 10,15 mm

Tebal benda uji (t)		= 10,40 mm

Panjang pendulum (R)	= 0,8 m

Berat pendulum (G)	= 30 kg x 9,8 = 294,3 N

Cos α			= 90º		= 0

Cos β			= 85,75º	= 0,0741

Mencari luas penampang:

Ao	= ℓ x t

= 10,15 x 10,40

= 105,560 mm2

Rumus energi yang diserap benda uji/tenaga patah:

E 	= G x R ( Cos β - Cos α )

E	= 294,3 x 0,8 ( 0,0741 – 0 )

E 	= 235,44 x 0,0741

E 	= 17,4 J

Rumus Harga Impak (HI):

HI	= EA

= 17,4105,560

= 0,164 J/mm2

- Menghitung fraksi berat baja AISI 1020 dan FeMn (1,5%, 2% & 2,5%).

- Pembuatan cetakan pasir

- Proses pengecoran

- Hasil cor

- Pengujian Spesimen

PT MAKMUR META GRAHA DINAMIKA

PT MAKMUR META GRAHA DINAMIKA

Doc. Control : 21/FF/4/TDS/0006

Technical Data Sheet

FERRO MANGANESE

HIGH CARBON

FUNCTION:

PT. MAKMUR META GRAHA DINAMIKA

H

ead Office :

W

ISMA 77 Tower II, 25

th

Floor.

J

l. Letjend. S. Parman Kav.77,

S

lipi, Jakarta Barat, 11410

P

hone

:

+62.21.2967 5888, 2967 5999

F

ax

:

+62.21.2967 5899, 2967 5988

W

ebsite

:

www.makmurmeta.co.id

E

mail

:

info@makmurmeta.co.id

PT. MAKMUR META GRAHA DINAMIKA

H

ead Office :

W

ISMA 77 Tower II, 25

th

Floor.

J

l. Letjend. S. Parman Kav.77,

S

lipi, Jakarta Barat, 11410

P

hone

:

+62.21.2967 5888, 2967 5999

F

ax

:

+62.21.2967 5899, 2967 5988

W

ebsite

:

www.makmurmeta.co.id

E

mail

:

info@makmurmeta.co.id

Alloying material pada saat melting

PRODUCT SPECIFICATION:

Mn

:

75% Min

Si

:

1.2% Max

C

:

7.5% Max

P

:

0.25% Max

S

:

0.03% Max

PACKING:

1

MT/JUMBO BAG

SIZE:

10

– 60 mm

PRODUCT SPECIFICATION:

Mn

:

75% Min

Si

:

1.2% Max

C

:

7.5% Max

P

:

0.25% Max

S

:

0.03% Max

PACKING:

1

MT/JUMBO BAG

SIZE:

10

– 60 mm

ALL MATERIALS IN THIS INFORMATION ARE INTELECTUAL PROPERTY OF PT. MAKMUR META GRAHA DINAMIKA